### PART 1 – GENERAL

  - SUMMARY

- This section includes the following:

- Bicycle Parking Racks (Shark™)

  - QUALITY ASSURANCE

- Installer Qualifications: An experienced installer who has completed installation of similar bicycle parking racks.

- Manufacturer Qualifications: Graber Manufacturing, Inc. is a skilled manufacturer of bicycle parking racks since 1989.

- Source Limitations: For consistent quality in appearance and physical properties obtain each product from Graber Manufacturing, Inc.

- Product Options: Drawings indicate size, shape and dimensional requirements of furnishings for the purpose of customer sourcing.

  - SUBMITTALS

- Product Data: Include physical characteristics such as materials, specifications and finish.

- Drawings: Show details including dimensions, materials, and options for each product.

- Samples for Verification: Finish samples of the color and type of powder coat will be provided upon request.

- Maintenance Data: For each product include the recommended methods for repairing damage to the powder coat and materials finish will be provided.

  - DELIVERY, STORAGE AND HANDLING

- Store product(s) in original undamaged packaging and containers until ready for installation.

- Handle powder coated product(s) with sufficient care to prevent any scratches or damage to the finish.

  - WARRANTY

A. 	Bicycle parking racks carry a one year manufacturer’s limited warranty against defects in materials and workmanship. The warranty period begins the date of invoice.

### PART 2 - PRODUCTS

  - ACCEPTABLE MANUFACTURERS

A.	Madrax, a division of Graber Manufacturing, Inc. 1080 Uniek Drive, Waunakee, WI 53597. Toll free phone: 800-448-7931. Local phone: 608-849-1080.

  - MATERIALS

- Powder Coating: Triglycidyl isocyanurate (TGIC) powder, a polyester coating. Coating is applied so that the thickness is 3.5 to 4.5 mils.

- Color as selected by architect from manufacturer’s full range of standard colors.

- Galvanizing: Standard specification for zinc (hot-dip galvanized) coatings on iron and steel products

  - Finish is bright in appearance for 6 to 12 months after processing.  The finish dulls to a matt grey after during this period of time.

  - The product will have vent holes to allow gases to escape a molten galvanize to enter internal spaces.

  - Surface quality will meet the American Galvanizing Association standards.

  - BICYCLE PARKING RACKS

- Shark™: The bicycle parking rack shall be the SHK-__-__-__ (insert double or single, number of bikes and finish selection). Manufactured by Madrax, a division of Graber Manufacturing, Inc.

  - Rack shall be constructed of 3/4” (19.1mm) diameter carbon steel round bar; 2” x 3” (50.8mm x 76.2mm) carbon steel angle; and 2” x 1” (50.8mm x 25.4mm) carbon steel “C” channel.

- Shark Up™: The bicycle parking rack shall be the SHU-__-__-__ (insert double or single, number of bikes and finish selection). Manufactured by Madrax, a division of Graber Manufacturing, Inc.

  - Rack shall be constructed of 3/4” (19.1mm) diameter carbon steel round bar; 2” x 3” (50.8mm x 76.2mm) carbon steel angle; and 2” x 1” (50.8mm x 25.4mm) carbon steel “C” channel.

  - REFERENCES

- Flat Bar

- ASTM A36 Carbon Structural Steel

## Round Bar

## ASTM A36 Carbon Structural Steel

- Tubing

  - ASTM A513 Electric-Resistance-Welded Carbon and Alloy Steel Mechanical Tubing

- Galvanizing

  - ASTM A123 Standard Specification for Zinc (Hot-Dip Galvanized) Coatings on Iron and Steel Products

- Stainless Steel

  - ASTM A312 Standard Specification for Seamless, Welded, and Heavily Cold Worked Austenitic Stainless Steel Pipes

PART 3 – EXECUTION

  - INSTALLATION

- Install in accordance with manufacturer’s instructions.

- Embedded mounting: Material is to be extended a minimum of 10” (254mm) below finish surface and cast in concrete.

- Surface mounting: Location and drilling of holes for inserts included.

- Some assembly required.